SECTION 32 1823

- PART 1 GENERAL

  - RELATED WORK

Related Sections: Review Contract Documents for requirements that affect work of this section. Specification sections that directly relate to work of this section include, but are not limited to:

Section 33 3000 – Site Improvements

Section 32 1826 - Synthetic Grass Surfacing

Section 32 1822 – Synthetic Athletic & Sports Surfacing

Section 12 9300 – Site Furnishings

Section 03 3000 – Cast-in-Place Concrete

Section 11 6500 – Athletic & Recreational Equipment

1.02	SUBMITTALS

A. Product Data: Submit manufacturer’s product literature, technical specifications, and other data required to demonstrate compliance with specified requirements for all athletic equipment.

1.03	QUALITY ASSURANCE

A. Fabrication and installation of site improvements by experienced craftsmen with excellent record of performance on completed projects of comparable size, scope, and quality.

B. All materials, hardware and furnishings shall be new, first quality.

1.04	FIELD MEASUREMENTS

A. Contractor shall verify position and layout of all athletic field equipment. Verify dimensions by field measurements.

1.05 SYSTEM DESCRIPTION: Prefabricated shock attenuation, storm water management and 	cooling underlayment for synthetic turf athletic fields, synthetic turf roof decks, and other synthetic 	turf applications.

PART 2: PRODUCTS

2.01 PREFABRICATED SHOCK ATTENUATION & WATER RETENTION PAD

A. BASE: Basis of specification: BlueLay as provided by:

SportsEdge®

P.O. Box 837

259 Murdock Rd.

Troutman, NC 28166

PH: 800.334.6057

FX: 704.528.0179

info@sportsedge.com

www.sportsedge.com

## B. COMPONENTS

1. Shock Attenuation and Water Retention Underlayment: BlueLay as supplied 			by SportsEdge, location as shown on plans, consisting of 97cm (38.2”) x 120cm 			(47.2”) panels fabricated of 100% mineral wool from basalt (32% recycled), with 			the following attributes:

a. Thickness: 30mm (1.2”)

b. Density: 17.6 lbs./ft3 for stability during installation

c. Weight: 1.76 lbs./ft²

d. Panel dimensions: 97cm (38.2”) x 120cm (47.2”) or 12.5 ft² per panel

e. Weight per panel: 22 lbs.

f. Linear thermal expansion: 0.00 in/ft/°C

g. Water storage capacity: 0.5 gal/ft²

h. Dimensional stability: >99.9%

i. Manufactured and warranted by DutchBlue

C. PERFORMANCE CHARACTERISTICS: BlueLay Shock Pad tested with crumb rubber

& sand infill turf:

a. G-Max: 104 (ASTM F355-16).

b. Critical fall height: 1.39M (ASTM F3146-18)

c. Force reduction: 69% (3189-17)

d. Vertical deformation: 9.2mm (3189-17)

e. Compressive Set: 95% rebound at 25% compression (ASTM D395-B)

f. Vertical flow rate: 67 in/hr (EN 12616)

g. Temperature Management: Wet – Category 1 (FIFA Test Method 14)

h. Water Retention: 273%

i. Warranty: 25 years.

## PART 3: EXECUTION

3.03 INSTALLATION / QUALITY ASSURANCE

1. Install per the manufacturer’s instructions and as indicated on the plans; or by a factory 	trained and authorized installer.

END OF SECTION