Section 33 4460 Synthetic Turf Shock & Drain Pad System

PART 1: GENERAL

1.01 RELATED WORK

Review Contract Documents for requirements that affect work of this section. Specification sections that directly relate to work of this section include, but are not limited to:

Section 03 1500 - Concrete Accessories

Section 22 1420 - Storm Drainage Piping

Section 31 2300 - Excavation and Fill

Section 32 1820 - Athletic & Sports Surfaces

Section 32 1826 - Artificial Grass Surfacing

Section 03 3000 - Cast-in-Place Concrete

Section 33 4000 - Storm Drainage Utilities

SYSTEM DESCRIPTION

Prefabricated shock attenuation and storm water drainage pad for synthetic turf athletic fields, synthetic turf roof decks and other synthetic turf applications.

PART 2: PRODUCTS

2.01 PRE-FABRICATED SHOCK ATTENUATION / DRAINAGE PAD

ACCEPTABLE MANUFACTURERS;

- Basis of specification: SportsEdge® Defender.14C™:

SportsEdge®

P.O. Box 837

259 Murdock Rd.

Troutman, NC 28166

PH: 800.334.6057

info@sportsedge.com

www.sportsedge.com

## B. COMPONENTS (Designer select one);

- Shock Attenuation Underlayment: Defender.14C as supplied by SportsEdge, location as shown on plans, consisting of 2.1 meter wide rolls with longitudinal drainage channels on bottom surface, fabricated of 100%  post-industrial recycled, open-cell polyurethane, with the following attributes:

- Density: 15 lbs/cubic foot minimum for stability during installation

- Thickness: 14mm

- Weight: 0.60 lbs/ft²

- Roll dimensions: 2.1 M (6.89 Ft) x 0.25.0 M (82.0 Ft)

- Linear thermal expansion: 0.00185 in/ft/°C

- Water storage capacity: 0.25 gal/ft²

- Dimensional stability: >99%

- Tensile strength: 35.9 lbs/in² (min)

- 100% recycled and recyclable

- Manufactured and warranted by Greiner Multifoam

C. PERFORMANCE CHARACTERISTICS

Defender.12 Shock Pad Tested per ASTM F355A with crumb rubber & sand infill turf:

    - G-Max: 107 (avg).

    - Critical fall height: 1.4M (avg)

    - Force reduction: 65.7% (avg)

    - Vertical deformation: 9.8mm (avg)

    - Energy restitution: 36.3% (avg)

    - Compressive strength: 16psi at 25% compression, 32psi at 50% compression, 145psi at 75% compression.

    - Vertical flow rate: 308 in/hr (ASTM 4491)

    - Horizontal flow rate: 68.7 gpm/ft at 0.5% slope (ASTM 4716)

    - Warranty: 25 years Minimum.

    - Manufacturer shall have a shock and/or drainage pad installed in a minimum of 100 sports fields.

    - Manufacturer shall have a minimum of ten (10) FIFA certified fields currently in use.

## PART 3: EXECUTION

3.03 INSTALLATION / QUALITY ASSURANCE

1. Install per the manufacturer’s instructions and as indicated on the plans; or by a factory trained and authorized installer.

END OF SECTION