Section 33 4460 Sub-drainage

PART 1: GENERAL

1.01 RELATED WORK

Review Contract Documents for requirements that affect work of this section. Specification sections that directly relate to work of this section include, but are not limited to:

Section 03 1500 - Concrete Accessories

Section 22 1420 - Storm Drainage Piping

Section 31 2300 - Excavation and Fill

Section 32 1820 - Athletic & Sports Surfaces

Section 32 1826 - Artificial Grass Surfacing

Section 03 3000 - Cast-in-Place Concrete

Section 33 4000 - Storm Drainage Utilities

SYSTEM DESCRIPTION

The geocomposite Panel Drain made from recycled materials should consist of the SportsEdge® HQ6 or SportsEdge® HQ12:

- Part # SEHQ6 - 	1“ x 6” for Natural Turf Fields, vertical installation

- Part # SEHQ12 - 	1“ x 12” for Synthetic Turf Fields, horizontal installation

PART 2: PRODUCTS

2.01 GEOCOMPOSITE SUBSURFACE DRAIN SYSTEM

ACCEPTABLE MANUFACTURERS:

SUBSURFACE DRAIN:

Base; SportsEdge® HQ12 as supplied by:

SportsEdge®

P.O. Box 837, 259 Murdock Rd.

Troutman, NC 28166

PH: 800-334-6057

info@sportsedge.com

www.sportsedge.com

## COMPONENTS

The two-part pre-fabricated system shall consist of a solid formed polystyrene perforated core fully wrapped with a non-woven spun-bound polypropylene filter fabric. The prefabricated drain core is to be made from recycled materials.

1. Core: Solid formed polystyrene

a. Length: 150 foot

b. Perforated

c. Widths: 6, 12, 18 or 24 inches

d. Depth: 1" minimum

e. Recycled material

2. Geotextile Fabric:

a. Non-woven spun-bound polypropylene filter fabric

b. Glue bonded to the core

3.  Accessories:

a. Couplers, Outlets, Geotextile End Caps as required and recommended by the manufacturer.

4. Subsurface drain system shall meet the following ASTM standards as a minimum.

| TECHNICAL DATA |  |  |  |
| --- | --- | --- | --- |
| Physical Property | Unit of Measure | Typical Value | ASTM Test Method |
| FABRIC |  |  |  |
| Grab Tensile | lbs | 145 | D 4632 |
| Grab Elongation | % | 60 | D-4632 |
| Puncture Resistance | lbs | 50 | D-4833 |
| EOS (AOS) | US Std Sieve | 70 | D-4751 |
| Flow Rate | gpm / ft² | 80 | D-4491 |
| CORE |  |  |  |
| Thickness | in | 1 | D-1777 |
| Compressive Strength | psf | 9,000 | D-1621 |
| Flow Capacity per unit width | gpm/ft | 21 | D-4716 |

## PART 3: EXECUTION

3.03 INSTALLATION

1. Install per the manufacturers recommendations, or as indicated on the drawings.

END OF SECTION