Section 33 4460 Precast Track Perimeter Channel Drain

PART 1: GENERAL

1.01 RELATED WORK

Review Contract Documents for requirements that affect work of this section. Specification sections that directly relate to work of this section include, but are not limited to:

Section 03 1500 - Concrete Accessories

Section 22 1420 - Storm Drainage Piping

Section 31 2300 - Excavation and Fill

Section 32 1820 - Athletic & Sports Surfaces

Section 32 1826 - Artificial Grass Surfacing

Section 03 3000 - Cast-in-Place Concrete

Section 33 4000 - Storm Drainage Utilities

SYSTEM DESCRIPTION

Track Surface to Turf Areas:

- System to be SportsEdge PRO-S Channel Drain System of one meter (1m) long drain channels, manufactured of Polymer Concrete with removable thermoplastic ADA compliant grates #336, grate locking devices, and accessories. Assembly number S-192.

Track Surface to Track Surface Areas:

- System of one meter (1m) long slot drain channels of polymer concrete and schedule 40     PVC pipe, in-line polymer concrete catch basins with removable covers, and accessories. The slot width shall not exceed 12mm” (7/16”), in compliance with ADA requirements. Assembly Number XT-4.

Assembly number: 1) S-192-336 	2) XT-4

PART 2: PRODUCTS

2.01 PRE-FABRICATED CHANNEL DRAIN

ACCEPTABLE MANUFACTURERS

Surface drain:

A. BASE: Shall be:

  - PRO-S Channel Drain, with #336 Thermoplastic ADA grates and grate locking devices; and

  - XT-4 Slot Drain as manufactured by:

SportsEdge®

P.O. Box 837, 259 Murdock Rd.

Troutman, NC 28166

PH: 800-334-6057

info@sportsedge.com

www.sportsedge.com

## B. COMPONENTS PRO-S CHANNEL DRAIN:

1.  PRO-S Channel: S-192 fabricated of polymer concrete, 6 inches wide, 4 inch ID and 8.625 inch deep minimum with radius non-sloping bottom having the following attributes:

a. Length: 1 meter (39.2 in).

b. Depth: shall be 8.625" minimum.

c. Anchoring ribs: Full Length.

d. Grate locking slots: blind, vibration dampening, thermoplastic.

e. Interlocking ends.

2. Grates: Fabricated of thermoplastic polymer.

- #2336 Herringbone Pattern:

- Meeting Heel proof (0.25”<) and

- ADA (0.5”<) requirements.

- 6.2 mm drainage openings.

- Color: Black (Alt. Designer select a color)

- Length: 1/2 meter (19.7")

- UV stabilizers

3.  Catch basins: #2900SE fabricated of polymer concrete

a. Width:  6" OD, 4" ID

b. Depth:  22.1"

c. Length: 1/2 meter (19.7")

d. Grate locking slots: blind, vibration dampening, thermoplastic.

C. COMPONENTS XT SLOT DRAIN

1. Drain Channel: #XT-4; location as shown on the plans, fabricated of polymer concrete, schedule 40 PVC pipe, 4 inch ID, with radius non-sloping bottom having the following attributes:

a. 12mm (15/32”) maximum width polymer concrete drainage slot with interlocking ends, with polymer concrete reinforcing at 6.25” intervals.

b. Overall Depth: 5.9375” OD (150mm)

c. Joint Coupler:

1. PVC Slip coupler, 3.75” minimum.

d. Length: 1 meter (39.19 in).

2 meter (78.38 in).

e. Radiused 1M Length: (R35.5M) if required.

2.  Catch basins: #2900XTA fabricated of polymer concrete.

a. Width:  6", 4" ID

b. Depth:  22.1"

c. Length: 1/2 meter (19.7")

d. Cover: polymer concrete, .12mm (7/16”) slot, removable.

e. Locking device for cover.

3.  Accessories: XTPC connector plate, fabricated of polymer concrete.

a. Pro channel drain / XT slot drain Connector, when required.

## PART 3: EXECUTION

3.03 INSTALLATION / QUALITY ASSURANCE

1. Install per the manufacturer’s instructions and as indicated on the plans; or by a factory trained and authorized installer.

END OF SECTION