Section 33 4460 Precast Track Perimeter Slot Drain

PART 1: GENERAL

1.01 RELATED WORK

Review Contract Documents for requirements that affect work of this section. Specification sections that directly relate to work of this section include, but are not limited to:

Section 03 1500 - Concrete Accessories

Section 22 1420 - Storm Drainage Piping

Section 31 2300 - Excavation and Fill

Section 32 1820 - Athletic & Sports Surfaces

Section 32 1826 - Artificial Grass Surfacing

Section 03 3000 - Cast-in-Place Concrete

Section 33 4000 - Storm Drainage Utilities

SYSTEM DESCRIPTION

System of two meter (2m) long and one meter (1m) long slot drain channels of polymer concrete and schedule 40 PVC pipe, in-line polymer concrete catch basins, and accessories. Slot width shall not exceed ½” (0.5”) in compliance with ADA requirements.

PART 2: PRODUCTS

2.01 PRE-FABRICATED SLOT DRAIN

ACCEPTABLE MANUFACTURERS; Surface drain;

- Base: shall be SportsEdge® XT-4 Slot Drain as manufactured by:

SportsEdge®

P.O. Box 837, 259 Murdock Rd.

Troutman, NC 28166

PH: 800-334-6057

info@sportsedge.com

www.sportsedge.com

## B. COMPONENTS

1. Drain Channel: #XT-4; location as shown on the plans, fabricated of polymer concrete, schedule 40 PVC pipe, 4 inch ID, 2 meter (78.38 in) lengths for the straight aways,1 meter (39.19 in) lengths for the track radius, with radius non-sloping bottom having the following attributes:

a. 12mm (15/32”) maximum width polymer concrete drainage slot with interlocking ends, with polymer concrete reinforcing at 6.25” intervals.

b. Overall Depth: 5.9375” OD (150mm)

c. Joint Coupler:

1. PVC Slip coupler, 3.75” minimum.

d. Length: 1 meter (39.19 in).

2 meter (78.38 in).

e. Radiused 1M Length: (R35.5M) if required.

2.  Catch basins: #2900XTA fabricated of polymer concrete.

a. Width:  6", 4" ID

b. Depth:  22.1"

c. Length: 1/2 meter (19.7")

d. Cover: polymer concrete, 12mm (15/32”) slot, removable.

e. Locking device for cover.

3.  Accessories: XT-4PC connector plate, fabricated of polymer concrete.

a. Pro channel drain / XT slot drain Connector, when required.

b. PVC end caps, when required.

## PART 3: EXECUTION

3.03 INSTALLATION / QUALITY ASSURANCE

1. Install per the manufacturer’s instructions and as indicated on the plans; or by a factory trained and authorized installer.

END OF SECTION